| SECTION | 705 |
| --- | --- |
| AGGREGATES FOR BITUMINOUS COURSES |

SCOPE

MATERIALS COVERED

This specification covers the quality and size of local mineral materials and commercial mineral fillers used in bituminous base and surface courses.

REQUIREMENTS

GENERAL

The mineral aggregate shall be the crushed and screened product of approved deposits.

The Engineer reserves the right to prohibit the use of aggregates from any source when:

The character of the material is such, in the opinion of the Engineer, as to make improbable the furnishing of aggregates conforming to these specifications; or

The character of the material is such, in the opinion of the Engineer, that undue additional costs may be accrued by the Contracting Agency; or

The maximum allowable water absorption of either coarse or fine aggregate exceeds 2.5 percent when tested in accordance with ASTM C127 (coarse aggregate) and ASTM C128 (fine aggregate).

The mineral aggregate shall be clean, hard, durable, and free from frozen lumps, deleterious matter, and harmful adherent coatings.

When producing plantmix aggregate, all natural fines passing the No. 4 sieve shall be screened from the coarse aggregate and may be reintroduced into the mix at a rate not to exceed 20 percent by dry weight of the combined aggregates.

The natural fines may be used only when all applicable mix design criteria have been met.

DEFICIENCIES

If the product of any deposit is deficient in the fraction passing the No. 50 sieve, additional filler from other approved deposits meeting the physical requirements may be added.

The added material shall be fed to the drier in a uniform manner from a separate stockpile.

If the added material is a commercial mineral filler, it shall be uniformly fed directly to the plant.  This shall not be construed as a waiver of any of the requirements contained herein.

PHYSICAL PROPERTIES AND TESTS

PLANTMIX AND ROADMIX BITUMINOUS BASE AND SURFACE AGGREGATE, TYPES TWO FINE AND COARSE AND THREE

The aggregate shall conform to this subsection.

Test specimens shall be prepared following dry preparation procedure described in ASTM D4318, Section 10.2 through Section 10.2.5.

| TABLE 1 – PLANTMIX AND ROADMIX AGGREGATE GRADATION |
| --- |
| Sieve Sizes | Percent By Weight Passing Sieve |
|  | Type 2 Coarse Arterials | Type 2 Fine Residential/Collector | Type 3 |
| 1-Inch | 100 | 100 | -- |
| 3/4-Inch | 84-97 | 90-100 | -- |
| 1/2-Inch | 66-82 | 78-94 | 100 |
| 3/8-Inch | 56-72 | 68-84 | 90-100 |
| No. 4 | 35-50 | 50-65 | 55-85 |
| No. 8 | 23-38 | 30-49 | 32-67 |
| No. 50 | 5-19 | 7-25 | 7-27 |
| No. 200 | 2-7 | 2-9 | 2-10 |

| TABLE 2 – PLANTMIX AND ROADMIX AGGREGATE SPECIFICATIONS |
| --- |
| Project Tests | Test Methods | Requirements |
| Sieve Analysis | AASHTO T27 | Above |
| Sampling Aggregate | ASTM D75 | -- |
| Fractured Faces | NEV. T230 | Traffic Category I: 90% Minimum (2 fractures minimum) 95% Minimum (1 fracture minimum) |
|  |  | Traffic Category II: 35% Minimum (2 Fractures minimum) |
| Plasticity Index | ASTM D4318 | All Traffic Categories: 6 Maximum |
| Liquid Limit | ASTM D4318 | All Traffic Categories: 35 Maximum |
| Methylene Blue Test | AASHTO TP57 | 10 Maximum |
| Fine Aggregate Angularity | AASHTO T304 | Traffic Category I: 45% |

| Source Tests | Test Methods | Requirements |
| --- | --- | --- |
| Stripping Test | ASTM D1664 | Satisfactory |
| Percentage of Wear (500 Rev.) | ASTM C131 | All Traffic Categories: 35% Maximum |
| Elongation @ 5:1 | ASTM D4791 | Traffic Category I: 10% Maximum |
| Soundness Test | ASTM C88 | All Traffic Categories: 8% Maximum |
| Deleterious Materials | ASTM C142 | All Traffic Categories: 0.3% Maximum |

BLANK

PLANTMIX BITUMINOUS OPEN-GRADED SURFACE AGGREGATE

The aggregate shall conform to the following requirements:

| TABLE 3 – OPEN GRADE AGGREGATE GRADATION |
| --- |
| Sieve Sizes | Percentage By Weight Passing Sieve |
| 1/2-Inch | 100 |
| 3/8-Inch | 90-100 |
| No. 4 | 35-55 |
| No. 8 | 5-15 |
| No. 200 | 0-3 |

| TABLE 4 – OPEN GRADE AGGREGATE SPECIFICATIONS |
| --- |
| Project Tests | Test Methods | Requirements |
| Sieve Analysis | AASHTO T27 | Above |
| Sampling Aggregate | ASTM D75 | -- |
| Fractured Faces | NEV. T230 | 90% Minimum (2 fractures minimum) |

| Source Tests | Test Methods | Requirements |
| --- | --- | --- |
| Percentage of Wear (500 Rev.). | ASTM C131 | 37% Maximum |

COMMERCIAL MINERAL FILLER

Commercial mineral filler shall conform to ASTM C977 for quicklime, ASTM C1097 for hydrated lime, and ASTM D3910 and ASTM D242 for slurry seal and microsurfacing.

Sampling of the mineral aggregate and mineral filler shall conform to AASHTO T2/‌ASTM D75 methods.

All aggregate shall be from the same source.

No field blending will be allowed.

When tested according to the following tests, the mineral aggregate shall meet the following requirements:

| TABLE 5 - MINERAL FILLER AGGREGATE GRADATION |
| --- |
| Property | Test Method | Specification |
| Sand Equivalent | AASHTO T176/‌ASTM D2419 | 50 Minimum for Slurry and 65 Minimum for Microsurfacing |
| Plasticity Index | ASTM D4318 | NP |
| Soundness, % | AASHTO T104/‌ ASTM C88 | 15 Maximum (using NA2SO4) |
| Abrasion Resistance, % | AASHTO T96/‌ASTM C131 | 30 Maximum. Abrasion test shall be run on the aggregate before it is crushed. |

When tested in accordance with AASHTO T27, AASHTO T11, ASTM C136, and ASTM C117, the mineral aggregate with mineral filler shall conform to the gradations indicated below.  Percentage passing shall not vary from the high limit to the low limit on any 2 consecutive sieves.

SCREENINGS

The screenings shall conform to the following requirements:

| TABLE 6 – SCREENINGS GRADATION |
| --- |
| Sieve Sizes | Percentage By Weight Passing Sieve |
|  | 1/2-Inch | 3/8-Inch |
| 1/2-Inch | 100 | -- |
| 3/8-Inch | 90-100 | 100 |
| No. 4 | 15-35 | 20-45 |
| No. 16 | 0-4 | 0-6 |
| No. 200 | 0-2 | 0-2 |

| TABLE 7 SCREENINGS SPECIFICATIONS |
| --- |
| Project Tests | Test Methods | Requirements |
| Sieve Analysis | AASHTO T27 | Above |
| Sampling Aggregate | ASTM D75 | -- |
| Fractured Faces | NEV. T230 | 90% Minimum (2 fractures minimum) |

| Source Tests | Test Methods | Requirements |
| --- | --- | --- |
| Percentage of Wear (500 Rev.) | ASTM C131 | 37% Maximum |

SAND BLOTTER

The sand shall conform to the following requirements:

| TABLE 8 – SAND BLOTTER GRADATION |
| --- |
| Sieve Sizes | Percentage By Weight Passing Sieve |
| 1/2-Inch | 100 |
| No. 4 | 90-100 |
| No. 16 | 30-75 |
| No. 200 | 0-12 |

| TABLE 9 – SAND BLOTTER SPECIFICATIONS |
| --- |
| Project Tests | Test Methods | Requirements |
| Sieve Analysis | AASHTO T27 | Above |
| Sampling Aggregate | ASTM D75 | -- |
| Organic Impurities | ASTM C40 | -- |

| TABLE 10 - ISSA, TYPE I GRADATION |
| --- |
| Sieve Size | Mix Design Range (Percentage By Weight Passing Each Sieve) | Stockpile Tolerance |
| 3/8-Inch | 100 | 0 |
| No. 4 | 100 | 0 |
| No. 8 | 90-100 | ±5% |
| No. 16 | 65–90 | ±3% |
| No. 30 | 40-65 | ±3% |
| No. 50 | 25-42 | ±3% |
| No. 100 | 15-30 | ±2% |
| No. 200 | 10-20 | ±2% |

| TABLE 11 - ISSA, TYPE II GRADATION |
| --- |
| Sieve Size | Mix Design Range (Percentage By Weight Passing Each Sieve) | Stockpile Tolerance |
| 3/8-Inch | 100 | 0 |
| No. 4 | 90-100 | ±5% |
| No. 8 | 65-90 | ±5% |
| No. 16 | 45-70 | ±3% |
| No. 30 | 30-50 | ±3% |
| No. 50 | 18-30 | ±3% |
| No. 100 | 10-21 | ±2% |
| No. 200 | 5-15 | ±2% |

| TABLE 12 - ISSA, TYPE III GRADATION |
| --- |
| Sieve Size | Mix Design Range (Percentage By Weight Passing Each Sieve) | Stockpile Tolerance |
| 3/8-Inch | 100 | 0 |
| No. 4 | 70-90 | ±5% |
| No. 8 | 45-70 | ±5% |
| No. 16 | 28-50 | ±3% |
| No. 30 | 19-34 | ±3% |
| No. 50 | 12-25 | ±3% |
| No. 100 | 7-18 | ±2% |
| No. 200 | 7-15 | ±2% |

SET CONTROL ADDITIVES

The type and quantity of additives in slurry seal and microsurfacing mix shall be determined by the material mix design and conform to the applicable sections of ASTM D3910 and ISSA T102.

PLANTMIX AND ROADMIX ASPHALT CONCRETE SURFACE COURSE UTACS TYPE S1 THROUGH S3

The Ultrathin Asphalt Concrete Surface (UTACS) shall use one of the gradation types listed below as required by the Engineer.

| Table 13 - Ultrathin Asphalt Concrete Surface (UTACS) Gradations |
| --- |
| Sieve Size | Type S1 | Type S2 | Type S3 | Tolerance |
| 3/4-Inch1 | -- | -- | 100 | -- |
| 1/2-Inch | -- | 100 | 85-100 | ±6 |
| 3/8-Inch | 100 | 85-100 | 60-80 | ±6 |
| No. 4 | 40-55 | 22-40 | 22–38 | ±4 |
| No. 8 | 19-32 | 19-32 | 19-32 | ±4 |
| No. 16 | 15-25 | 15-23 | 15-23 | ±3 |
| No. 30 | 10-18 | 10-18 | 10-18 | ±3 |
| No. 50 | 8-13 | 8-13 | 8-13 | ±3 |
| No. 100 | 6-10 | 6-10 | 6-10 | ±3 |
| No. 200 | 4-7 | 4-7 | 4-7 | ±2 |

Coarse aggregate testing shall comply with Table 2.  Coarse aggregate is defined as aggregate that is retained on and above the No. 4 sieve.

| Table 14 UTACS Coarse Aggregate Specifications |
| --- |
| Tests | Method | Limit |
| Los Angeles abrasion value, % loss | AASHTO T96 | 35 Maximum |
| Soundness, % loss | AASHTO T104 | 18 Maximum |
| Magnesium Sulfate or Sodium Sulfate | AASHTO T104 | 12 Maximum |
| Flat & Elongated Ratio, % @ 3:1 | ASTM D4791 | 25 Maximum |
| % Crushed, single face | ASTM D5821 | 95 Minimum |
| % Crushed, Two or more Mechanically crushed faces | ASTM D5821 | 85 Minimum |
| Micro-Deval, % loss | AASHTO TP58 | 18 Maximum |

For the Los Angeles abrasion value, the values shown for these tests are targets for aggregate selection purposes.  The results of these tests should not be the sole basis for rejection.

Fine aggregate testing shall comply with Table 3.

| Table 15 - UTACS Fine Aggregate Specifications |
| --- |
| Tests | Method | Limit |
| Sand Equivalent | AASHTO T176 | 45 minimum |
| Methylene Blue (on materials passing 200) | AASHTO TP57 | 10 maximum |
| Uncompacted Void Content | AASHTO T304 | 40 minimum |

Values for sand equivalent shown for these tests are targets for aggregate selection purposes.  If the finished bituminous mixture passes the AASHTO T283 requirement in the Mix Design section, the sand equivalent and methylene blue requirements may be waived.